## Slide 1
BASF 3D Printing Solutions (B3DPS)
Status October 2022
Ultracur3D® RG 3280
Product Launch Package

## Slide 2
Ultracur3D® Photopolymer Solutions – Our product lines
Flexible
Tough
Rigid
Dental
Supplementary
Daylight

## Slide 3
Ultracur3D® RG 3280
Material Introduction
Ultracur3D® RG 3280 is the first composite material we are adding to our rigid product line. Due to the high loading of ceramic particles, this material has an extremely high stiffness around 10 GPa and an HDT B above 280°C.
These outstanding properties place it in an exceptional position among our other resins. Moreover, despite the high particle loading, the viscosity is kept low and the settling of particles is limited, making this resin very easy to handle and print. Its high stiffness and temperature resistance make this the perfect material for tooling, molding and wind tunnel testing.
The material has a white, ceramic-like color and feel.

## Slide 4
Ultracur3D® RG 3280
Value Proposition
Ultracur3D® RG 3280:
Ceramic-filled resin with exceptionally high stiffness and temperature resistance
Superior stiffness
Superior temperature performance
Very fast and easy to print
High suspension stability
Color: White, ceramic-like
General availability: 11/2022
* This is only a general indication for compatibility, as there is a very wide range of different printers available in the
market. If you have any question about machine compatibility, contact us at sales@basf-3dps.com
NOTE: Due to higher density of the resin an adjustment in the filling volumes was made.
Current filling volumes: 1l (=1.65kg) and 5l (=8.25kg)
Young’s modulus | 10,000 MPa
Tensile strength | 76 MPa
Elongation at break | 1 %
HDT (0.45 MPa) | >280 °C
HDT (1.82 MPa) | 132 °C
Viscosity, 30 °C | 230 mPas
Available color(s) | White, ceramic-like
Compatible technologies* | DLP, LCD

## Slide 5
Ultracur3D® RG 3280
Benchmarking
 | RG 35 | RG 1100 | RG 3280 | Competitor product
Young’s modulus | 2,600 MPa | 3,080 MPa | 10,000 MPa | 10,500 MPa
Tensile strength | 80 MPa | 70 MPa | 76 MPa | 68 MPa
Elongation at break | 6 % | 5 % | 1 % | 1.1 %
HDT (0.45 MPa) | 83 °C | 116 °C | >280 °C | 132 °C
HDT (1.82 MPa) | 64 °C | 84 °C | 132 °C | 82 °C
Viscosity, 30 °C | 600 mPas | 201 mPas | 230 mPas | 1,000 mPas
Despite the high loading of ceramic particles, this material is low viscous and very easy to handle and print.
Combined with a significantly higher temperature resistance than Ultracur3D® RG 35 and Ultracur3D® RG 1100, while maintaining a comparable tensile strength, it’s a novel material perfectly suitable for tooling, molding and wind tunnel testing.
Compared to an existing product on the market, Ultracur3D® RG 3280 shows a better performance in temperature resistance and tensile strength combined with a significantly lower viscosity.
Additionally, its superior stiffness, high suspension stability and slow settling in the vat make this material very easy to handle while fulfilling the printing requirements of our customers.

## Slide 6
Ultracur3D® RG 3280
Certifications & Post-Processing
Chemical resistance
UV resistance
Sterilization
  Testing planned.
  Not tested.
  Not tested.
  Testing planned.
Bio compatibility

## Slide 7
Ultracur3D® RG 3280
Example of Suitable 3D-Printers and Settings
Evaluation on additional systems ongoing.
Further details can be found in the User Guideline.
PRINTER | MIICRAFT ULTRA 125 | PHROZEN SONIC MINI 4K | NEXA3D XiP | NEXA3D NXE
Wavelength | 405 nm | 405 nm | 405 nm | 405 nm
Power | 2 mW/cm2 | 1.2 mW/cm2 | Print parameters available by Nexa3D | 3 mW/cm2
Curing time | 1.75 s | 2.1 s | Print parameters available by Nexa | Print parameters available by Nexa
Voxel depth | 100 μm | 50 μm | 100-200 μm | 100-200 μm

## Slide 8
NOTE: All MSDS are only initial and will not be updated in this presentation.
However, the links to the rest of the documents are always up-to-date. We recommend to use them instead of downloading the documents.
Ultracur3D® RG 3280
Available Documents
* MSDS available for the following countries:
US, CA, MX, EU, DE, AT, CH, BE, NL, LU, FR, ES, GB, IT, PL, CZ, DK, CN, TW, JP, KR, AU, NZ, MY, SG, BR
TDS
Not yet available.
MSDS*
User Guideline
Certifications
Pictures
TDS_Ultracur3D_RG 3280
Pictures_
Ultracur3D_RG 3280
UG_Ultracur3D_RG 3280

## Slide 9
Ultracur3D® RG 3280
Battle card
Material overview
FAQ
Target industries
Example of suitable 3D printers
Can the polymer be burnt out afterwards to create a 100% ceramic part?
No, this material is meant to be used in the form of a plastic with ceramic filler.
What is the ceramic loading in this material?
The ceramic loading in this material is around 65 wt%.
Is a thermal postcure necessary?
No, just a UV postcure is sufficient. A thermal postcure can be added optionally to enhance the HDT properties, as indicated on the TDS.
Ultracur3D® RG 3280 is a ceramic-filled resin with exceptionally high stiffness and temperature resistance. The material is characterized by:
Superior stiffness
Superior temperature performance
Very fast and easy to print
High suspension stability
Novel ceramic-filled resin ensuring easy handling and printing
Its unique properties guarantee good suspension stability and low settling in the vat
The material is especially suitable for applications where high stiffness and temperature performance are required
Thanks to its high stiffness and temperature resistance this material perfectly fulfills all customers’ requirements for tooling, molding and wind tunnel testing applications.
  MiiCraft - Ultra 125P
  Phrozen - Sonic Mini 4K
  Nexa3D – XiP and NXE
Key features

## Slide 10
We enable our customers
to shape the Additive Manufacturing industrial revolution.
Our Mission

## Slide 11
Ultracur3D® RG 3280
Contact Details
At Forward AM we strive to provide you with the best service possible.
If you have questions about our materials, technologies or services, or would like to request an expert consultation, we will be delighted to hear from you!
Any questions left?
Let’s talk!
www.forward-am.com
sales@basf-3dps.com
+49 6221 67417-900
linkedin.com/company/basf-forwardam