## Slide 1
BASF 3D Printing Solutions (B3DPS)
Status March 2024
Ultracur3D® SLA 7700
SLA | General-Purpose | Ultraclear
Product Launch Package

## Slide 2
Ultracur3D® Photopolymer Solutions – Our product lines
Flexible
Tough
Rigid
Dental
SLA
Daylight
Supplementary

## Slide 3
Ultracur3D® SLA 7700
Material Introduction
Ultracur3D® SLA 7700 is a versatile material specifically designed for easy and reliable processing on large-vat Stereolithography (SLA) machines.
The combination of exceptional clarity, with excellent accuracy and processing speed makes this material ideal for aesthetic and functional prototypes in a multitude of industries ranging from consumer goods to automotive and aerospace.

## Slide 4
Ultracur3D® SLA 7700
Value Proposition
Ultracur3D® SLA 7700:
General-purpose SLA resin, easy-to-print and exceptional part clarity
Exceptional optical clarity
Easy and reliable printing on large-vat systems
Excellent accuracy, detail and surface finish
Color: Ultraclear
General availability: April 2024
Appearance | Ultraclear
Young’s Modulus | 2250-2550 MPa
Tensile Strength | 46-51 MPa
Elongation at Break | 5-15%
Impact Strenght (Izod) | 25 J/m
HDT (0.45 MPa) | 51°C
HDT (1.82 MPa) | 50°C
Water Absorption (24h) | 0.36%
Viscosity at 30°C | 330 mPas

## Slide 5
Ultracur3D® SLA 7700
Benchmarking
 | RG 35 | ST 45 | SLA 7700 | Competitor resin 1 | Competitor resin 2
Appearance | Clear | Clear | Ultraclear | Ultraclear | Ultraclear
Young’s Modulus | 2600 MPa | 2300 MPa | 2250-2550 MPa | 2270-2640 MPa | 2270-2470 MPa
Tensile Strength | 80 MPa | 60 MPa | 46-51 MPa | 46-53 MPa | 43-48 MPa
Elongation at Break | 6% | 25% | 5-15% | 3-15% | 5-8%
Impact Strenght (Izod) | 23 J/m | 30 J/m | 25 J/m | 40-58 J/m | 25 J/m
HDT (0.45 MPa) | 83°C | 73°C | 51°C | 51°C | 50°C
HDT (1.82 MPa) | 64°C | 61°C | 50°C | 50°C | 49°C
Water Absorption (24h) | 0.33% | >5% | 0.36% |  | 0.35%
Viscosity at 30°C | 600 mPas | 210 mPas | 330 mPas | 250 mPas | 300 mPas
Ultracur3D® SLA 7700 is a versatile material specifically designed for easy and reliable processing on large-vat SLA machines.
In comparison to other materials in our portfolio, like Ultracur3D® ST 45: It has slightly lower HDT, but much lower water absorption as well. Compared to Ultracur3D® RG 35, it has overall similar mechanical properties but has a nicer part clarity and slightly higher elongation at break.
Compared to existing products on the market, Ultracur3D® SLA 7700 shows overall a similar performance.
Please do NOT publish this data. This is not allowed according to European law.
confidential
DO NOT PUBLISH

## Slide 6
Ultracur3D® SLA 7700
Certifications & Post-Processing
  Testing ongoing. Results available soon.
Bio compatibility
  Testing ongoing. Results available soon.
Chemical resistance
  Testing ongoing. Results available soon.
UV resistance
  Not tested.
Sterilization

## Slide 7
Ultracur3D® SLA 7700
Example of Suggested Printer Settings*
Here the suggested range of basic printing parameters. Based on the size of laser beam, hatching parameters, print parameters will vary. Please always refer to the user manual of the employed 3D printer for instructions on printer settings and handling.
Further details can be found in the User Guideline.
 | PRINTER SETTINGS
Wavelength | 355 nm
Dp | 5 mils / 0.127 mm
Power | 150-300mW
Beam size | 0.06-0.1mm
Hatching Speed | 6000 – 10000mm/s
Contour Speed | 3500-5500mm/s
Support Speed | 800-1200mm/s
* This is only a general indication for compatibility, as there is a very wide range of different printers available in the
market. If you have any question about machine compatibility, contact us at sales@basf-3dps.com

## Slide 8
NOTE: All MSDS are only initial and will not be updated in this presentation.
However, the links to the rest of the documents are always up-to-date. We recommend to use them instead of downloading the documents.
Ultracur3D® SLA 7700
Available Documents
* MSDS available for the following countries:
US, CA, MX, EU, DE, AT, CH, BE, NL, LU, FR, ES, GB, IT, PL, CZ, DK, CN, TW, JP, KR, AU, NZ, MY, SG, BR
TDS
Not yet available.
MSDS*
User Guideline
Certifications
Pictures
Extended TDS_Ultracur3D_SLA 7700
UG_Ultracur3D_SLA 7700
Pictures_
Ultracur3D_SLA 7700

## Slide 9
Ultracur3D® SLA 7700
Battle card
Material overview
FAQ
Target industries
Suitable 3D printer examples
Can this material be printed on DLP/LCD printers (385-405 nm)?
No, this material is especially designed for SLA systems (355 nm) and will not print well on DLP/LCD.
My SLA machine is closed, can I still use this material?
Probably yes, you can try printing it with existing settings for clear prototype materials. Please reach out to us for more information.
Can this material be used for investment casting?
This will depend on the exact requirements and casting process, please reach out to us for more info.
Why do we have a range in TDS for SLA resin?
Due to chemistry of the material, the polymerization remains active up to several days, thereby changing the mechanical properties. Therefore, values will be different if you measure it on day one or day three. Although we have observed after two days the values to be closer to one mentioned in TDS.
Ultracur3D® SLA 7700 is a general-purpose SLA resin, easy-to-print with exceptional part clarity. The resin is characterized by:
Exceptional optical clarity
Easy and reliable printing on large-vat systems
Excellent accuracy, detail and surface finish
Novel SLA resin with well-balanced mechanical perfor-mance
Minimal material shrinkage makes the resin perfect for printing large parts
Ultracur3D® SLA 7700 is suitable for a wide range of application, especially requiring exceptional part clarity
The combination of exceptional clarity, accuracy and processing speed makes this material ideal for aesthetic and functional prototypes in a multitude of industries ranging from consumer goods to automotive and aerospace.
  The material is specifically designed for easy and reliable processing on large-vat Stereolithography (SLA) machines.
  Working wavelength: 355 nm.
Key features

## Slide 10
We enable our customers
to shape the Additive Manufacturing industrial revolution.
Our Mission

## Slide 11
Ultracur3D® SLA 7700
Contact Details
At Forward AM we strive to provide you with the best service possible.
If you have questions about our materials, technologies or services, or would like to request an expert consultation, we will be delighted to hear from you!
Any questions left?
Let’s talk!
www.forward-am.com
sales@basf-3dps.com
+49 6221 67417-900
linkedin.com/company/basf-forwardam